Accurate Measurments of fine displacements

by analysis  of speckle patterns

M. Nicklawy(1), M. Bahrawi, A. F. Hassan(1) and N. Farid*

(1)Helwan university, Science faculty, Physics dpt.

National institute for standards (NIS), Tersa st.,

Haram, Giza, Egypt

(* Author for corresponding; E-mail: niveenfarid@yahoo.com)

### Abstract

One of the non-destructive techniques which provide examination of objects and materials without affecting their future usefulness is the speckle photography technique. Speckle photography is a technique for making moderate sensitivity measurements for strain, rotation, vibration, in-plane, and out-of-plane displacements. Its principle attractions are simplicity of optical system and the relative ease of displaying and interpreting the results. This paper discusses the determination of the displacements of the surface points by digital processing of speckle photography and by studying the speckle patterns correlation and visibility considering the effect of the object surface roughness.

Keywords :  Fine displacement;  speckle visibility;  correlation; Digital fourier transform

# Introduction

Since the advent of lasers, special attention has been paid to the study of scattering  phenomena of their highly coherent light. The random intensity distribution "speckle pattern" in the scattered light field from a rough surface has especially been studied by many workers and had become one of the most  important research subjects  in coherent optics. In conjunction with  fundamental studies  of speckle pattern, a wide variety  of its applications  has been proposed and actually used in the field of scientific and industrial measurements [1, 3]. One of the scientific and industrial measurements is fine displacement of a specific object [2].  In electronic speckle correlation method, coherent light illuminates a rough surface, the diffracted waves from each point of the surface mutually interfere to form a pattern which appears as a  grain pattern  of bright and dark regions [4, 5].   The degree of correlation of two speckle patterns produced from the same surface by two different illumination beams can be used  in determination of object displacement.  So as the object is illuminated  by a monochromatic plane wave  with an angle  of incidence  with respect to  the normal to the surface and multi-scattering and shadowing effects are neglected, the photo-sensor of a CCD camera placed  in the focal plane  of a Fourier  lens is used  for recording speckle patterns [6].  The Fourier transform technique  is considered to be one of the most attractive techniques for fine displacement  measurement., because of the direct relationship between the fourier transform spectrum and the displacement made by the object. The visibility of the resulted interference patterns are strongly affected by the surface texture of such object [7].  In this paper,  digital fourier transform  DFT  is used to measure the displacement of such object using the effect of  its surface roughness  on the  pattern visdibility and correlation. The accuracy of the proposed method depends on the resolution of the imaging system.

## In plane displacement

Let f(x,y) expresses the height distribution function over a selected area  A  and  h is the average  height given by

h=1Af(x,y) dx dy

where f(x,y) can be expressed as:

f(x,y)=a1 sin2πλ1x+y+a2 sin2πλ2x+y+...

The surface roughness is defined by:

Ra=1Af(x,y)−h dx dy

According to the electromagnetic wave propagation theory, the scattering of light from rough specimen is determined  by the diffraction phenomena. The amplitude function of the wavefront reflected  by such surface  having  the height distribution function f(x,y) is presented by:

A(x,y)=eiφ(x,y)

in which the phase function is defined as

φ(x,y)=2πλ×2f(x,y) cosθ

where  is the wavelength  of the light source, 1 is the incident angle.

The fourier transform of the existing wavefront  f(x,y) is

w(f1,f2)=A(x,y) exp−2πiλ(f1x+f2y) dx dy        (1)

where f1  and  f2  are the spatial frequencies and

f1=XML             and              f2=YML

L is the focal length of the transform lens,  M  is the magnification  of the system and  X,Y are the coordinates on the image plane.  Using the expansion of the exponential function f(x,y) and ignoring the constants, equation (1) becomes:

w(f1,f2)=n=1∞Cnif(x,y)nn! exp−2πiλ(f1x+f2y) dx dy     (2)

where  Cn  are the constants  of the expansion:

Cn=4πcosθλn

for small (x,y)</10,  the first term of the right hand side  of equation (2)   at n=1 is predominant and this is the case of smoothness, for large (x,y),  the second term is significant.  The profile of a symmetrical spectral line can be designed by:

g(υ)=g(υ0) exp−4ln2(υ−υ0)2δυ2

where  0: is  the frequency at the origin, : is the spectral half width.

The intensity of the speckle patterns at single exposure  is

I1=w(f1,f2) w∗(f1,f2)g(υ) dυ

after displacement the intensity  will  be    I2   and the total intensity after  the double exposure  I=I1+I2  .The visibility of the interference patterns  will be

V=Imax−IminImax+Imin

## Experimental setup

The proposed method involves the use of a light source He-Ne laser of wavelength 0.633µm. The object is placed on a traveling micrometer to allow capturing images for the object at different positions as shown in figure 1.

Figure 1: Setup of measuring displacement

The pattern is captured  by a CCD camera before and after displacement and the two images are stored and added  digitally. Computer software is used to produce Fraunhofer diffraction pattern of the surface.  The Specimens used in this work are of surface roughness values 1.57, 3.1, 4.5, 6.25µm. The specimens are displaced for 20, 40, 80, 100 µm. The visibility of the interference fringes is affected by the surface roughness of each specimen at every displacement  as shown in figures  2 and 3. Figure 4 shows that,  the contrast  of the speckle patterns decreases  as  both  of the   surface  roughness  and the

surface  lateral displacement increases.

Figure2: Interference fringes  and relative intensity distribution of the specimens

(a)1.57,  (b)3.1, (c)4.5, (d)6.25µm at displacement  20µm.

Figure 3:Interference fringes and relative intensity distribution  of the specimens   (a)1.57,  (b)3.1, (c)4.5, (d)6.25µm at displacement 100µm.

Figure 4:  Contrast  at different in-plane displacements for different surfaces

## Out of plane displacement

The degree of correlation of two speckle patterns produced  from the same object can be analyzed .  The object is illuminated  by a coherent plane wave  emerging  from a He-Ne laser.  Double exposures obtained at two different positions are recorded successively on the same image respectively.

The consequence    of varying the location of the object has two folds:

- the speckle pattern is translated in a direction corresponding to  the object displacement   (),

- the correlation between the first and the second  speckle  pattern decreases by increasing the object displacement.

This correlation depends on the roughness of the object. Digital fourier transform DFT is applied to the recorded speckle patterns, and Young fringes are produced. The fringe visibility is lower than unity because the two speckle patterns are not fully correlated.  The visibility is a decreasing function of the displacement  and the surface roughness Ra. The measurement of the visibility  V   will lead to measuring   displacement. Figure 5 shows the geometrical definitions  mentioned   in the paper.

The object surface  of  f(x,y)  is illuminated with coherent plane wave  of incidence  1 And the scattering angles are denoted  by  2 and 3, k1  is the propagation vector  of the incident  beam and  k2  is the propagation vector of the scattered  beam.  vx, vy, and vz  are the cartesian  components of (k1-k2).

The scattered  field  A2    is given by:

A2=AFSexp(i(vxx+vyy+vzf(x,y))) dx dy                     (3)

this equation has been established in [4].

A: the reflected  filed , F: the geometrical factor, S: area of the surface.

For simplification, the deviation will be limited to one-dimension and   equation (3) will be rewritten as:

A2=AF2l−l+lexp(i(vxx+vzf(x,y))) dx dy

Figure 5:  geometrical definitions

2l:  the width of the pupil of the surface

vx=2πλ sinθ1−sinθ2

vz=2πλ cosθ1−cosθ2

the recording system is assumed to be located near the normal to the surface  S.  Using the approximation   sin2 2 u/h, the field  A2(u) at the point u on the  recording system is given by:

A2=AF2lp(x)exp(i(ksinθ1x+vzf(x))) exp(−i(kh)ux) dx

where  k=2π/λ,  and  p(x) is the pupil function. Put

F(x)=p(x) expi(ksinθ1x+vzf(x))

where F(x) is  the complex amplitude at any point  of the surface derived from the Fresnel approximation. The intensity E(u),  during  the first exposure is then:

E(u)=A2(u)2

and during the second exposure

E'(u)=A'2(u)2

where

A'2(u)=AF2lF'(x) exp(−i(kh)ux) dx

F'(x)=p(x)exp(i(ksinθ'1x+v'zf(x)))

The fourier transforms are elevated  at  frequencies u/λh in the recording system plane and  ω/λ d  in the fourier plane. Choosing h=d, ω is the real coordinate in the fourier plane. The intensity along ω is then given by [4]:

E(ω)=A(ω)2=A2F24l22I(vz,vz)+I(v'z,v'z)+2I(vz,v'z)cos(2kcosθ1δ ω)

The general solution of this equation leads to Young fringes of which the spatial frequency  is (2 cosθ1 δ )/λ,  and the visibility  of the fringes is given by:

V=2I(vz,v'z)I(vz,vz)+I(v'z,v'z)                            (4)

<I(vz,vz)>   and  <I(v’z,v’z)>  represent the power spectral density functions of each  speckle pattern.  The term  <I(vz,v’z)> is a  function of the correlation between  the two speckle patterns  where  the correlation coefficient  C(τ)   decreases from its maximum value  C(0)=1  to  C(∞)=0.      τ=x1-x2   is the separation parameter.  The correlation distance T is  defined  in [4]  in which  C(τ)  drops to the value  e-1.  For  τ > T,  C(τ)  is very small. The term  <I(vz,v’z)> can be described as:

I(vz,v'z)=e−(vz−v'z)2σ2πT22vz v'z σ212

substituting in  equation (4)

V=2e−σ2(vz−v'z)2(vzv'z)12vz+v'z                      (5)

since  vz- v’z≈(2 π) /λ sinθ1 δ,  the equation (5) becomes

V≈e−((2πλ)σsinθ1δ)2

# Experimental work

Different standard specimens are used in this experiment whose average surface  roughness are 1.6, 2.3, 3.17, 4.5, 6.3µm, every specimen is illuminated at different angles θ. The light source used in illumination is He-Ne laser of λ=0.632µm. The CCD camera  [Cohu 3810 model] is placed at (p) in the field of observation to record the speckle. The object is shifted slightly by out-of-plane displacement δ, and the speckle patterns are recorded at each δ. The FFT is applied digitally to the recorded speckle patterns to obtain Young fringes in the Fourier plane (figures 6 and 7).

Figure 6: Young's fringes for surfaces of  Ra (a) 1.6µm, (b) 3.17µm at δ1  .

Figure 7: Young's fringes for surfaces of  Ra (a) 1.6µm, (b) 3.17µm at  δ2.

The visibility of Young fringes is calculated for each specimen at different out-of-plane displacement δ. The values of -ln V are plotted in figure 8  as a function of δ2 for different  surface roughness.

Figure 9: Relation between δ2 and  -lnV at  θ =160.

### Accuracy  of the  measurement

Since the following conditions must be satisfied in the proposed methods:  the surface is perfectly conducting,  multiple scattering and shadowing effects  have been neglected, the incident wave  is plane and  linearly  polarized, and the Fraunhofer approximation  is used.   Then the  accuracy of  such  method  depends on the following factors:  the light source used in illumination,  effect of the environment,  accuracy of  the surface roughness values, resolution of the imaging system CCD camera, and repeatability of measurements.

# Conclusion

A simple method is proposed to measure fine in-plane displacement of different objects having different roughness values using digital Fourier transformation of the speckle pattern recorded on a CCD camera at different locations. The measured values are plotted against the visibility of the interference fringes. Fine out-of plane displacement is studied by analysis of the correlation of two speckle pattern and a relation between the visibility and the displacement is demonstrated.

### References

1. Francon, M., “Laser speckle and applications in optics”, Academic press, (1979).

2. Francon, M., Koulev, P., and May, M., “Detection of small displacement of diffuse objects illuminated by a speckle pattern”, Optics communications, 15(2), (1975).

3. Jones, R. and Wykes, C.,  “Holographic and speckle interferometry”, Cambridge university press, Cambridge, (1989).

4. Beckmann P. and Spizzichino A., “The scattering of electro magnetic waves from rough surfaces”, (Pergamon, New Yourk, 1963).

5. Dainty, J. C., “Laser speckle and related phenomena”, springer verlag, second edition, (1984).

6. Gad~G. M., “Interferometric studies of two correlated diffusers”, Thesis, Helwan university, Egypt, (1993).

7. Goodman, J. W.,   “Dependence of image speckle contrast on surface roughness”, Opt. comm., 14, 323--327, (1975).